DALVEN products

CAPE TOWN:   
     P.O. Box 371,  
Eppindust
 7475
Tel:  021 593 6790
Fax:  021 593 8650
JOHANNESBURG:      P.O. Box 1358,   
Florida   
 1710   
Tel:  011 472 4417   Fax:  011 472 1206
HEAD OFFICE:    
     P.O. Box 26738, Hout Bay 
 7872   
Tel:  021 790 2379   Fax:  021 790 3360

E-mail: info@dalven.co.za




    Website: www.dalven.co.za

BITUMEN ADHESIVE

DESCRIPTION
Cutback bitumen adhesive contains selected bitumens, solvents and fillers, blended to give optimum drying and laying times.  Product consistency is controlled to give easy spreading and optimum coverage.

TYPICAL USES

Cutback flooring adhesive is ideal for bonding vinyl asbestos floortiles, roofing felt, and wooden blocks onto smooth and dry cement floor screeds or slabs.

SURFACE PREPARATION

Ensure that the surface is dry.  Very porous or mildly dusty surfaces should first be primed with a single brush or roller application of Bituminous Priming solution.  The prime coat should be allowed to dry before applying the adhesive.

APPLICATION
1. Spread cutback bitumen adhesive with a notched trowel.  Ensure that the triangular notches in the trowel are of sufficient depth (usually 1.5mm).

2. Allow the adhesive to dry till only a slight pick-up is evident with moderate finger pressure.  This tacky stage will be reached 15 - 20 minutes after application.  The adhesive is now ready to receive the covering.

3. Adhesive that has dried excessively and which will not stain the finger pressed into it with moderate pressure must be scraped off and a fresh layer applied.

4. Do not risk laying the tiles, woodblocks or roofing felt on a freshly applied layer of the adhesive.  The covering material may be displaced during the initial wet stage if laid too soon.

Warning

Flammable product.  Cutback bitumen adhesive contains a volatile flammable solvent.  Apply the adhesive only in a well ventilated area and taking necessary fire precautions.  Keep containers closed and store away from heat, sparks and open flames.

SPECIFICATION
Product type :



Solvent based bituminous adhesive.

Colour :



Black.

Spread rate :



4.0 - 7.0 sq. m. per litre.

Drying time (to tacky stage) :

15 - 20 minutes in a well ventilated area.

Application temperature :

5 - 30 degrees C.

Flash point :



20 degrees C.

Mass per litre :


0.99kg.































DALVEN products cc;     Registration Number: 1997/ 004076/23;     VAT Number: 4720163015
Member: A.D.J. Swanepoel B.Sc.Eng., M.B.A.


