DALVEN products

CAPE TOWN:   
     P.O. Box 371,   Eppindust   7475
Tel:  021 593 6790
Fax:  021 593 8650
JOHANNESBURG:      P.O. Box 1358,   Florida   1710   
Tel:  011 472 4417   Fax:  011 472 1206
HEAD OFFICE:    
     P.O. Box 26738,   Hout Bay   7872   
Tel:  021 790 2379   Fax:  021 790 3360

E-mail: info@dalven.co.za




    Website: www.dalven.co.za

HOT- APPLIED CRACK SEALER

DESCRIPTION

Hot-applied crack sealer is a bitumen which has been modified with a high percentage of an elastomeric polymer.  Once it has cooled it becomes highly elastic.  It will not soften or flow at high ambient temperatures and will not crack at low temperatures.
TYPICAL USES

It is suitable for filling cracks or joints in asphalt or concrete surfaces.

SPECIAL FEATURES

Water and detritus is prevented from getting into joints or cracks.

Movement in joints can be accommodated by the elastic behaviour of the product.

SURFACE PREPARATION

Clean out all dust and debris from the joint or crack. (If possible with a high pressure air hose).

Apply weed killer if required.

Ensure that the crack or joint is dry before pouring the hot product.

APPLICATION

1. Heat the product in the tin to a temperature of approximately 150oC or until it acquires a free flowing consistency.

2. Using a suitable pot, or kettle with a spout, carefully pour the hot product into the crack. until the cracksealer reaches the level of the surfaces adjacent to it.

3. Wear appropriate protective clothing and take precautions while working with hot product.

SPECIFICATION

Property




Test value

Test Method
Ring and ball softening point


65 - 80 min.

ASTM D36

Ductility at 10oC (mm)



500 min.

ASTM D113

Elastic recovery at 10oC (%)


80 min.

ASTM D113 (mod)

Flow at 60oC (mm)



0


BR4T


AVAILABILITY
5 litre, 20 litre and 200 litre metal containers or 20kg paper bags.






























DALVEN products cc;     Registration Number: 1997/ 004076/23;     VAT Number: 4720163015
Member: A.D.J. Swanepoel B.Sc.Eng., M.B.A.


