DALVEN products

CAPE TOWN:   
     P.O. Box 371,   Eppindust   7475
Tel:  021 593 6790
Fax:  021 593 8650
JOHANNESBURG:      P.O. Box 1358,   Florida   1710   
Tel:  011 472 4417   Fax:  011 472 1206
HEAD OFFICE:    
     P.O. Box 26738,   Hout Bay   7872   
Tel:  021 790 2379   Fax:  021 790 3360

E-mail: info@dalven.co.za




    Website: www.dalven.co.za

 SOUND DEADENING COMPOUND
DESCRIPTION

DALVEN Sound Deadening Compound is a soft, non-flowing product based on bitumen emulsion containing selected non-abrasive fillers.

TYPICAL USES
DALVEN Sound Deadener dramatically reduces noise levels on corrugated roof sheets, metal panels or pressings such as those found in the sheet metal and automotive industries.

After application to the inside of car floor and door panels, underneath car wings, kitchen sinks etc.,  the dried film will considerably reduce the noise level due to car body vibration and similarly the handling of domestic utensils and cutlery on stainless steel sinks.  Application to metal roof sheets dramatically reduces noise levels resulting from rain or hail.

SURFACE PREPARATION AND APPLICATION
The compound may be applied to clean, rust free surfaces by means of a brush. A single application of 1.0 - 1.5 litres per m2 area is normally required.  For a greater film thickness, apply two coats of 1 litre per m2 each.  When applying to new galvanised sheets ensure that any protective coating of oil has been removed with a suitable detergent or solvent. 

DALVEN Sound Deadening Compound is ready for application as supplied, but if desired, the viscosity of the product may be reduced by the addition of a small quantity of water.  Drying period will be a few hours, depending on interior conditions and ventilation of the work area.  The wet material when first applied, can be damaged by water, but once dried, a tough bituminous film is formed that will resist abrasion.  Cleaning can be done with water while the product is wet.  Once dry, use paraffin to clean brushes and equipment.

DALVEN Sound Deadening Compound, being water based, is non-flammable and the cured film has a restricted flame spread.

SPECIFICATION

Product type:  
                       Water based highly filled bitumen emulsion

Colour:                                    Dark brown

Coverage:                               1.0 - 1.5 litre/m2 average

Drying time:                             2-3 hours outdoors

Flash Point:                             Non-flammable

Fire Resistance                       Low fire spread

Mass per litre:                         1.2 kilograms

Availability:                              5 litre, 20 litre, 200 litre containers.






























DALVEN products cc;     Registration Number: 1997/ 004076/23;     VAT Number: 4720163015
Member: A.D.J. Swanepoel B.Sc.Eng., M.B.A.


