DALVEN products

CAPE TOWN:   
     P.O. Box 371,  
Eppindust
 7475
Tel:  021 593 6790
Fax:  021 593 8650
JOHANNESBURG:      P.O. Box 1358,   
Florida   
 1710   
Tel:  011 472 4417   Fax:  011 472 1206
HEAD OFFICE:    
     P.O. Box 26738, Hout Bay 
 7872   
Tel:  021 790 2379   Fax:  021 790 3360

E-mail: info@dalven.co.za




    Website: www.dalven.co.za

ACRYLIC COMPOUND

DESCRIPTION

Acrylic Compound is a brushable acrylic coating material which can be used to create high quality, long lasting waterproofing systems, and to protect against the effect of ultra-violet rays.

TYPICAL USES

Acrylic Compound was specifically developed for use as a decorative and protective coating to be used in waterproofing applications.  It can be used in multiple layers together with geotextile fabric to create a durable and flexible waterproof membrane.

Suitable for use on flashings, parapets and flat concrete roofs.  

SPECIAL CHARACTERISTICS

  * High resistance to degradation by ultra-violet rays

  * Flexible under all ambient temperatures

  * Easy to apply

  * Available in five colours

  * Excellent hiding power

  * Thixotropic - resists flow on vertical surfaces

  * Resists fungus and mould growth

APPLICATION

PURE ACRYLIC WATERPROOFING SYSTEM    Prime the surface with Acrylic Compound diluted 50/50 with water.  Apply Acrylic Compound at 1litre per m2 and immediately imbed geofabric into the wet layer.  Apply saturation coat of Acrylic Compound onto the fabric at 0.7 litre per m2.  Apply final coat of Acrylic Compound at right angles to the saturation coat at a rate of 0.7 litres per m2.  Allow each layer to dry for at least 3 hours before applying the following coat.

NOTES:

  i)   Do not apply if rain is imminent

 ii)   Brushes and rollers should be washed in clean water immediately after use

iii)   Acrylic Compound has an optimum consistency.  If necessary, dilute with water.

SPECIFICATION

Product type:

Water based pigmented acrylic emulsion compound

Colour:


White, grey, green, black and red

Coverage:

Approximately 3.5 sq. m. per litre on a smooth surface

Finish:


Medium sheen

Density:

1.3 kg per litre

Viscosity:

100 -120 Kreb units (Soft paste)

Solid content:

60% m/m minimum

Flash point:

None

Artificial weathering:
No defects after 2000 hours in weatherometer. SABS method 182

Availability:

1 litre, 5 litre, 20 litre and 200 litre containers.






























DALVEN products cc;     Registration Number: 1997/ 004076/23;     VAT Number: 4720163015
Member: A.D.J. Swanepoel B.Sc.Eng., M.B.A.


