DALVEN products

CAPE TOWN:   
     P.O. Box 371,  
Eppindust
 7475
Tel:  021 593 6790
Fax:  021 593 8650
JOHANNESBURG:      P.O. Box 1358,   
Florida   
 1710   
Tel:  011 472 4417   Fax:  011 472 1206
HEAD OFFICE:    
     P.O. Box 26738, Hout Bay 
 7872   
Tel:  021 790 2379   Fax:  021 790 3360

E-mail: info@dalven.co.za




    Website: www.dalven.co.za

BITUMINOUS ALUMINIUM PAINT

DESCRIPTION
Bituminous Aluminium Paint consists of specially refined bitumen, solvents and aluminium pigment.  These have been scientifically blended to give a paint having a bright aluminium finish, good drying characteristics, and offering lasting protection.

TYPICAL USES

Bituminous Aluminium Paint can be applied to metal roofs, mastic roofing, roofing felt, bituminous compounds, asbestos cement sheets and tiles, structural steel, piping, storage tanks etc.  The bright aluminium finish reflects light on roofs, and the painted film protects the metal from corrosion.

SURFACE PREPARATION

Remove all dust , dirt, and rust with a wire brush or broom and inspect to ensure that the surfaces have been thoroughly cleaned.  Grease and anti-white rust treatment (some galvanised surfaces) should also be removed.  Absorbent surfaces such as concrete, asbestos cement or timber should first be primed with Priming Solution and the coat allowed to dry before painting.

Previously corroded metal surfaces require special attention.  These should first be cleaned and then treated with rust inhibitors (such as phosphate treatments) and then primed with Bituminous Priming Solution before overcoating the dried film with Bituminous Aluminium Paint.  Roofing mastics, roofing felt and new bituminous surfaces should be allowed to weather for 4-6 weeks before applying Bituminous Aluminium Paint.

APPLICATION
1.  Stir the contents of the container well before use.

2.  Bituminous Aluminium Paint can be applied by brush, roller or spray gun and the 

     coverage varies from  5-8 m2 per litre per coat, depending on the surface texture of

     the substrate.  It is recommended that two coats be applied; the second after allowing

     the first to dry for 2-3 hours, on a sunny day.

3.  Wet aluminium paint is flammable, and naked flames should not be allowed in the

     work area.  Adequate ventilation should be provided when working in closed areas.

4.  Do not apply if the surface is less then 2oC above dew point, or below 5oC or 

     above 50oC.

NOTES
 a)   Close the container securely when not in use.  If thinning is required, use mineral

        turpentine or paraffin.  

 b)    Brushes or spraying equipment can be cleaned in mineral turpentine or paraffin.

 c)   Occasionally, thermal movement in thin bituminous coatings may cause superficial

       crazing in bituminous aluminium coatings.  This can be prevented by first applying

       an undercoat of white acrylic paint, allowing  to dry before applying Bituminous

       Aluminium Paint.  Alternatively the product can be applied together with a fine

       reinforcing membrane.

SPECIFICATION
Product type:                                                   Bituminous Aluminium Paint.

Colour:                                                             Bright aluminium.

Coverage:                                                        5-8 m2 per litre on bituminous surfaces.  On metal surfaces 



  12-14 m2 at 60 micron.

Drying time:                                                     2-3 hours @ 25oC.

Flexibility; 4mm mandrill, 180 degree

bend:                                                               No cracking

Flash Point:                                                     42.5oC.

Mass per litre:                                                 0.95 kg.

Availability:
                                                1 litre, 5 litre, 20 litre, 200 litre






























DALVEN products cc;     Registration Number: 1997/ 004076/23;     VAT Number: 4720163015
Member: A.D.J. Swanepoel B.Sc.Eng., M.B.A.


