DALVEN products

CAPE TOWN:   
     P.O. Box 371,  
Eppindust
 7475
Tel:  021 593 6790
Fax:  021 593 8650
JOHANNESBURG:      P.O. Box 1358,   
Florida   
 1710   
Tel:  011 472 4417   Fax:  011 472 1206
HEAD OFFICE:    
     P.O. Box 26738, Hout Bay 
 7872   
Tel:  021 790 2379   Fax:  021 790 3360

E-mail: info@dalven.co.za




    Website: www.dalven.co.za

BITUMEN WATERPROOFING LIQUID

DESCRIPTION

Bitumen Waterproofing Liquid is a black waterproofing compound of brushable consistency that will adhere to all clean surfaces, damp or dry.

TYPICAL USES

Waterproofing Liquid will seal small cracks on parapet walls, flashings, concrete or metal roofs, ceramic tiles, plastered walls, etc.  When used together with reinforcing fabric such as a geotextile membrane, it provides an efficient and long lasting repair.

SPECIAL CHARACTERISTICS

The film will resist rain immediately after application and remains pliable on drying.  Waterproofing Liquid will also adhere to damp surfaces enabling urgent repairs to be made where necessary.

SURFACE PREPARATION

Remove all dust, dirt and rust.  Where there is moss and lichen etc., this should be removed, and the surface treated with fungicide which should be allowed to dry before further treatment proceeds.

APPLICATION

1.  Waterproofing Liquid can be applied to dry or damp surfaces; brush all excess water from wet  

     surfaces,  wipe with a cloth and apply.

2.  Applications can be made by means of a brush or knife blade.

3.  Durable repairs can be made by bedding a strip of geotextile fabric into the first Waterproofing  

     Liquid layer and overlapping the imperfection by about 35 mm all round, allowing to dry for a  

     period of a few hours, and then applying a second layer of Waterproofing Liquid.

4.  When used for sealing joints between roofs and surrounding walls, the treatment should be 

     taken 50 mm up the wall and 50 mm onto the roof surface and covered with Waterproofing   

     Liquid.

NOTES:

· 5 litres of Waterproofing Liquid will cover an area of  2.5m2 at a thickness of 2mm.

· Tools used to apply Waterproofing Liquid can be cleaned with paraffin or white spirits (mineral turpentine).

· Oil-based paint should not be applied over a freshly painted and dried film of Waterproofing Liquid as discolouration will result.  Allow at least two months weathering before painting.  

· Where the Waterproofing Liquid film will be exposed to the effects of ultra violet light, paint over  with bitumen aluminium paint or sealing compound.

SPECIFICATION

Product type:                Solvent based bituminous compound  containing 

                                     mineral fillers.

Colour:                         Black

Coverage:                    1.5-2.0 litres/m2 average.

Drying time:                 Touch dry 3-4 hours @ 25oC.

Flash point:                  43oC.

Mass per litre:              1.03  kilograms

Availability:                  1 litre, 5 litre, 20 litre, 200 litre containers































DALVEN products cc;     Registration Number: 1997/ 004076/23;     VAT Number: 4720163015
Member: A.D.J. Swanepoel B.Sc.Eng., M.B.A.


