DALVEN products

CAPE TOWN:   
     P.O. Box 371,  
Eppindust
 7475
Tel:  021 593 6790
Fax:  021 593 8650
JOHANNESBURG:      P.O. Box 1358,   
Florida   
 1710   
Tel:  011 472 4417   Fax:  011 472 1206
HEAD OFFICE:    
     P.O. Box 26738, Hout Bay 
 7872   
Tel:  021 790 2379   Fax:  021 790 3360

E-mail: info@dalven.co.za




    Website: www.dalven.co.za

BITUMEN MASTIC

DESCRIPTION

Bitumen Mastic is a black heavy bodied bituminous compound containing synthetic fibre for added strength.

TYPICAL USES

Before carrying out overall waterproofing it is essential to ensure that all cracks, holes and joints (other than hairline cracks, pinholes and other minor imperfections) are effectively sealed.  Bitumen mastic is specially formulated for this purpose and is trowel applied.  It can also be used in many other applications such as the repair of enlarged bolt holes, the sealing of laps on corrugated roofs, and sealing of joints in gutters.

SPECIAL CHARACTERISTICS

Bitumen Mastic will adhere to damp surfaces to permit urgent and essential repairs to be made.  It will resist rain immediately after application and remains pliable thereby accommodating thermal movement in buildings.

SURFACE PREPARATION

Remove all dust, dirt and rust and other loose material with a wire brush.

APPLICATION

1.  Apply Bitumen Mastic by trowel or knife at a thickness of at least 2mm so that it   

     overlaps adjoining surfaces by approximately 50mm on either side.

2.  As each repair is made, preferably lay a reinforcing strip of geotextile fabric, metal

    foil, canvas or thin roofing felt into the mastic,  bedding the edges in well.  The

    reinforcing should overlap the imperfection by at least 35mm all round.

3.  Cover the reinforcing strip with a thick protective coating of Bitumen Mastic.

4.  When used for sealing joints between roofs and surrounding walls, the treatment

     should be taken  50mm up the wall and 50mm onto the roof.  The reinforcing strip

    should then be dressed down the wall, over the joint and on to the roof surface and

    covered with a liberal amount of mastic.

NOTE:


a)   5 litres of Bitumen mastic covers an area of 2.5m2 at 2mm thickness.


b)   Where necessary, application can be made easier by dipping the trowel

                  occasionally in white spirits or paraffin.

c)   Tools used with Bitumen Mastic can be cleaned with paraffin or white
       spirits.

d) Oil-based paint should not be applied over Bitumen Mastic as
discolouration will result. Allow at least 2 months for weathering before painting over.

SPECIFICATION

Product type:

Solvent based bituminous compound containing mineral fillers and 


fibre

Colour:


Black

Coverage:

2.0 litres per m2 average

Flash point:

52oC

Mass per litre:

1.1kg

Availability:

1 litre,   5 litre,  20 litre and 200 litre containers .






























DALVEN products cc;     Registration Number: 1997/ 004076/23;     VAT Number: 4720163015
Member: A.D.J. Swanepoel B.Sc.Eng., M.B.A.


