DALVEN products

CAPE TOWN:   
     P.O. Box 371,  
Eppindust
 7475
Tel:  021 593 6790
Fax:  021 593 8650
JOHANNESBURG:      P.O. Box 1358,   
Florida   
 1710   
Tel:  011 472 4417   Fax:  011 472 1206
HEAD OFFICE:    
     P.O. Box 26738, Hout Bay 
 7872   
Tel:  021 790 2379   Fax:  021 790 3360

E-mail: info@dalven.co.za




    Website: www.dalven.co.za

BITUMINOUS PRIMER

DESCRIPTION
Bituminous Primer is a black, quick drying, low viscosity primer for concrete, asbestos cement, brick and similar masonry surfaces.  It is also an effective primer on metal surfaces such as steel, galvanised sheeting, aluminium etc.

After drying it leaves a non-sticky surface at normal air temperatures.

SURFACE PREPARATION

Surface must be clean and dry.

Remove excess loose or powdery material with a stiff brush or broom.  Cementitious surfaces must be free or laitance.

APPLICATION

Bituminous Primer can be sprayed or applied with a soft brush.  The coverage per litre on average masonry surfaces will be approximately 3-4 m2.

Drying time will be approximately 3-4 hours at 20oC.  At the end of this period the surface will be touch dry, but the surface should be allowed to dry for 24 hours before applying waterproofing or sealing compounds, as solvent entrapment will lead to poor adhesion.

CAUTION
Bituminous Primer contains volatile solvents and is inflammable.  Keep away from open flames.  The usual fire precautions should be taken when work is in progress.

SPECIFICATION
Product type:                                

 
Solvent based bituminous primer

Colour:                                          


Black

Coverage:                                    


0,2 - 0,3 litres per m2
Drying time:                                


3-4 hours at 20oC

Flash point:                                    


40oC (Typical)

Mass per litre:                                


0,88 kilograms

Viscosity:                                       


100 cSt at 25oC (typical)

Penetration of residue after distillation  to   360oC :
19 (100 grams/5 sec/25oC)

Availability:                                    


5 litre, 20 litre, 200 litre containers.































DALVEN products cc;     Registration Number: 1997/ 004076/23;     VAT Number: 4720163015
Member: A.D.J. Swanepoel B.Sc.Eng., M.B.A.


